## Slide 1: Measuring the wetting properties of cyclopentane hydrates
Fanny Thomas1, Jeffrey Morris1 and Didier Dalmazzone2
1 The Levich Institute and Department of Chemical Engineering,
The City College of New York
2 ENSTA ParisTech, Unité Chimie et Procédés
PIRE Annual Review Meeting
June 17th, 2019
Research Thrust 2: Formation and Control of Gas Hydrate Slurries

## Slide 2
Zylyftari et al. Chem. Eng Sci. 2013
Motivation
The crucial role of wetting and capillary forces
0% conversion – Water-in-oil emulsion
~70% conversion - 3-phase system
100% conversion - Suspension
Knowledge of the interfacial energy between hydrates and oil-field liquids is of great importance

## Slide 3
CP
DI Water
Methods
Initial plan
Measurement methods
Rigid, flat and smooth layer
Slow growth
As few crystals as possible
Experimental setup
Surface properties measurements:
Pendant drop method for interfacial tension
Contact angle on sitting drops
Droplet deposition
Contact angle
Hydrate layer
CP
Water

## Slide 4
1 – Formation of a flat hydrate surface

## Slide 5
Hydrate at CP/ Water interface:
Uniform coverage but neither smooth nor flat - pinning
Hydrate forming compound: Cyclopentane C5H10
Forms at atmospheric pressure, stable for T < 7°C
Only grows at the interface when no surfactant
Nucleation can be initiated by: seeding (by ice or hydrate), stirring, temperature variations
Once CP has evaporated
Non-rigid layer, mushy texture
CP
Hydrate layer
(Inside) DI Water
CP
DI Water
Goal: Rigid, flat and smooth layer
DI Water
Hydrate crystals floating
Formation of a flat CP hydrate surface
A challenging process

## Slide 6
CP
CP
Ice + CP
CP
Ice + H + CP
H (unpacked)
Freeze
+ Flip
Pack + Flip
T° cycles
+ overnight rest
H smooth and rigid
DI water + H + CP
CP
A very thin layer of ice is formed in liquid CP at -20°C. Hydrate nucleation is initiated by slowly raising the temperature above ice melting point.
Chart: Time (hours)
1
Ice melting initiating hydrate formation at the interface
Hydrate layer growing
2
3
Flip the
hydrate+ice sample
Hydrate formation
on the other side
Rest overnight for the layer to develop
4
Formation of a flat CP hydrate surface
Final procedure

## Slide 7
Tests conducted on the surface
The sample is left at rest in the cabinet above 0°C for several hours to check for stability and residual ice.
Contact angle measurements are also conducted on ice for comparison purposes.
Brine
With this method, we consistently obtain a flat, smooth and rigid hydrate surface (no ice).
The hydrate layer often needs to be packed before the last flipping step.
Side used for droplet deposition
T=2°C
Formation of a flat CP hydrate surface
Results

## Slide 8
2 – Surface properties of cyclopentane hydrates

## Slide 9
Criteria
One aqueous phase
(DI Water or Brine)
Ideally oil-field liquids
Non miscible
Should not degrade the hydrate surface (OH groups prohibited)
Contact angle measurement depends on the density ratio of the two liquids
hydrate
hydrate
1 Asserson, R. B., Hoffmann, A. C., Høiland, S., & Asvik, K. M. (2009). Interfacial tension measurement of freon hydrates by droplet deposition and contact angle measurements. Journal of Petroleum Science and Engineering, 68(3-4), 209-217.
2 Brown, E. P., Hu, S., Wells, J., Wang, X., & Koh, C. A.. "Direct measurements of contact angles on cyclopentane hydrates." Energy & fuels 32.6 (2018): 6619-6626.
Previous work
Asserson et. al. (2009), Norway 1
Freon hydrates
Chlorinated hydrocarbons / Water systems
Finite contact angle, water wet
Brown et. al (2018), Colorado School of Mines 2
Cyclopentane hydrates
Cyclopentane / Water system
Finite contact angle of θ=94.2° +/- 8.5°
=> Skeptical about this non intuitive result
Surface properties of cyclopentane hydrates Choice of the liquid/liquid systems

## Slide 10: Surface properties of cyclopentane hydrates Choice of the liquid/liquid systems
1 Asserson, R. B., Hoffmann, A. C., Høiland, S., & Asvik, K. M. (2009). Interfacial tension measurement of freon hydrates by droplet deposition and contact angle measurements. Journal of Petroleum Science and Engineering, 68(3-4), 209-217.
2 Brown, E. P., Hu, S., Wells, J., Wang, X., & Koh, C. A.. "Direct measurements of contact angles on cyclopentane hydrates." Energy & fuels 32.6 (2018): 6619-6626.
 | Surrounding Fluid | Droplet phase
1 | Brine | Dichloromethane
2 | Brine | 1,2-Dichloroethane
3 | Brine | Chloroform
4 | Cyclopentane | DI-Water
5 | Olive Oil | Brine
6 | Pumping Oil | Brine
7 | Silicone Oil | Brine
8 | Air | All of the above
Selected systems
Previous work
Asserson et. al. (2009), Norway 1
Freon hydrates
Chlorinated hydrocarbons / Water systems
Finite contact angle, water wet
Brown et. al (2018), Colorado School of Mines 2
Cyclopentane hydrates
Cyclopentane / Water system
Finite contact angle of θ=94.2° +/- 8.5°
=> Skeptical about this non intuitive result

## Slide 11
Chart: Measurement #
 | 131.24 | 131.24 | 70.16 | 45.82 | 39.4 | 38.1 | 38.58 | 37.57 | 38.96 | 39.18 | 38.88 | 38.99 | 36.48 | 35.07 | 28.72 | 26.02 | 23.83 | 20.46 | 19.17 | 15.77
A droplet of DI water (V=20µL) is deposited on the hydrate surface, immersed in CP. It spreads out almost completely before turning into hydrate. Temperature is about 1.5C° in the bath.
t=1s
t=7s
Water puddle turns into hydrate
CP
In contrast with previous work, we find that the hydrate surface is totally wetted by water when immersed in cyclopentane.
Brown et. al 1 Θ = 94.2° +/- 8.5°
Our work: total wetting Θ close to 0°
1 Brown, E. P., Hu, S., Wells, J., Wang, X., & Koh, C. A.. "Direct measurements of contact angles on cyclopentane hydrates." Energy & fuels 32.6 (2018): 6619-6626.
CP
CP
CP
CP
Surface properties of cyclopentane hydrates Cyclopentane / Water system

## Slide 12
Finite contact angles were obtained with brine as the surrounding phase and chlorinated hydrocarbons as the droplet phase.
Contact angle measurements were averaged over:
Multiple droplets for each substrate (tilting of the surface)
Right and left contact angle for each droplet (pinning and hysteresis)
Different hydrate surfaces, over time
Dichloromethane
1,2 - Dichloroethane
Chloroform
Surface properties of cyclopentane hydrates Chlorinated Hydrocarbons

## Slide 13
We obtained the interfacial tension between the droplet phase and the surrounding phase using the pendant drop method.
Young’s law
Young-Dupré equation
where is the work of adhesion
Droplet phase | Contact Angle | Interfacial Tension (mN /m) | From Young’s law (mN /m) | Work of adhesion (mN /m)
Dichloromethane | 149° | 27.9 +/- 0.1 | - 23.9 | 4.0
1,2-Dichloroethane | 140° | 26.5 +/- 0.2 | - 20.3 | 6.2
Chloroform | 125° | 27.7 +/- 0.1 | -15.9 | 11.2
Liquid 2
Liquid 1
Surface properties of cyclopentane hydrates Chlorinated Hydrocarbons

## Slide 14
Surrounding phase | Droplet phase | 
Brine | Dichloromethane | 149°
Brine | 1,2-Dichloroethane | 140°
Brine | Chloroform | 125°
Cyclopentane | DI-Water | 0°
Oils (olive, pumping, silicone) | Brine | 0°
Air | All of the above | 0°
Brine
T=2°C
Hydrate
Systematic and robust procedure to create cyclopentane hydrates with a smooth and rigid surface
New information on the wetting properties of cyclopentane hydrates
The aqueous phase totally wets the surface
Any liquid vs. air totally wets the surface
The aqueous phase preferentially wets the surface ( >90°).
Chloroform has the highest affinity for the hydrate surface
Conclusions

## Slide 15
Thank you for your attention!
Questions?

## Slide 17
Tests conducted on the surface
The sample is left at rest in the cabinet above 0°C for several hours to check for stability and residual ice.
Contact angle measurements are also conducted on ice for comparison purposes.
Hydrate layers
CP
Residual water+hydrate
Hydrate surface
Formation of a flat CP hydrate surface: Results
No apparent residual water if the ice layer is thin enough to start with.
Brine
With this method, we consistently obtain a flat, smooth and rigid hydrate surface (no ice).
The hydrate layer often needs to be packed before the last flipping step.
Side used for droplet deposition
T=2°C

## Slide 18: Formation of a flat hydrate surface: some pictures
Pack + Flip
Overnight rest
Ice immersed in CP
First layer of hydrate
at interface
Slow melting
T > 0°C
Hydrate layer on other side grows over T cycles
Next day: sometimes the hydrates grew wild!
Final state
Freeze underlying water layer then flip the hydrate+ice sample